# Acier ternaire faiblement allie au cr, mo ,v : caracterisation et evolution des carbures au cours de differents traitements thermiques

| Type Document | Thèses / mémoires |
| --- | --- |
| Langue | Français |
| Auteur(s) | Djoudi; Farheddine/ Boutefnouchet, Abdelatif/ Université Badji Mokhtar/ |
| Nombre de Pages | 72 f. |
| Illustration | tab., fig. |
| Format | 30 cm |
| Notes Générales | Bibliogr. Résumé en français, anglais et arabe |
| Diplôme | Magister |
| Etablissement | Annaba |
| Année de Soutenance | 2009 |
| Sujet(s) | précipitation/ austénitisation/ dilatométrie/ |

### Résumé :

The structural evolutions of a ternary high mechanical resistant steel (nuance 40CDV13) have been

approached by the characterization of its receipt state. In this state the studied steel presents a

structure composed of ferrite, pearlite and bainite. The primary carbides initially present in this state

are essentially M23C6, M7C3, MC and Fe3C. The dissolution of the cementite and the M23C6-type

carbide, in the austenitic matrix, is observed at 950 °C, the one of the M7C3 carbide intervenes from

1050 °C. The carbides of MC-type dissolve from 1100 °C which is translated by a very important

evolution of the austenitic grain size.

The precipitation of secondary carbides during four different continuous coolings, after a 10 minute

austenitization to 950°C, has been followed by X-ray diffraction on residues extracted from the

samples by an electrolytic process at the end of each cooling. This precipitation relates to cementite

and M23C6 carbide type. For a cooling speed of Vr = 75 °C/h ,there is prevalent precipitation of the

cementite which is attenuate thereafter, as the cooling rate become lower, giving rise to the

precipitation of carbide M23C6 For Vr = 25 °C/h , the precipitation of cementite considerably has

decreased and only primary MC and secondary M23C6 carbides remained and attest by the XRD

diffraction